# Nittobo      Gun Roving for Spray-Up

### Gun Roving is manufactured from a collection of continuous glass filaments gathered, without twists, into a single bundle. ### The strands which make up the bundle are bonded with polyester compatible size, then wound on a cylindrical package. Gun roving is designed for use in a variety of spray up processes and in a wide range of applications.

Product Code Indication    :    RS 240A-673WC                Properties

･ RS                          Roving Strand                                                ･ Fast wet-out and wet-through

･ 240                          linear weight of roving (TEX= g/1000m)  ･ Good choppability

･ A                                manufacturing classification                      ・ Good distribution

･ 673                          type of sizing                                                  ・ No fuzz

･ WC                          packaging specification

Technical Characteristics    (nominal values)

| Designation |  | Filament Diameter µm |  | Strand Treatment | Roving Tex / Yield | Loss on Ignition % |  | Moisture Content % | Wet out sec. | Applicable Resin |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RS 240A-673 |  | 11 |  | Silane | 2400 / 206 | 1.0 |  | Max 0.2 | 90 | Polyester |
| RS 240FG-625 |  | 11 |  | Silane | 2400 / 206 | 1.0 |  | Max 0.2 | 120 |  |
| RS 240FG-630 |  | 11 |  | Silane | 2400 / 206 | 1.0 |  | Max 0.2 | 60 |  |
| * other types in accordance with the agreement. |  |  |  |  |  |  |  |  |  |  |
| Packaging specifications |  |  |  |  |  |  |  |  |  |  |
| Weight (kg / lb) | Diameter (cm / in) |  | Height (mm / in) |  | Number of layer |  | Number of rovings in a layer |  | Number of rovings on a pallet |  |
| 18.0 / 40.0 | 28.0 /11.0 |  | 28.0 /11.0 |  | 3 |  | 16 |  | 48 |  |
| *Pallet dimensions (L x W x H / mm) 1110 x 1110 x 930 |  |  |  |  |  |  |  |  |  |  |

*Net weight of a pallet  (approximately / kg) 864

Storage

The roving should preferably be stored dry in their original packaging. The best conditions are at a

temperature between 10-35 C°℃ and at a 50-75% relative humidity level.

NITTO BOSEKI CO., LTD.              1-2-1, Nihonbashi Hama-cho Chuo-ku, Tokyo 103-8489, JAPAN

FRP SERVICES EUROPE

Parc de la Duranne – 235 Avenue L. de Broglie – 13857 Aix-en-Provence cédex 3 – France

Tel :+33 (0)442 97 59 10    Fax :+33 (0)442 97 59 20        web : http//www.frpservices.com        e mail :info@frpservices.com